## Slide 1: College of Engineering Department of Civil Engineering
The Design of a Highway Section of Alhofuf Western Ring Road in Alahsa
Fall 2020-2021 – Learning Outcome Assessment III
Final Presentation

## Slide 2: The Design of a Highway Section of Alhofuf Western Ring Road in Alahsa
Presented by:
  Nimran Alajmi 201602885
  Mohab Arafat 201502522
  Hassan Alkhunizi 201502170
  Ahmed Aleid 201500078
Supervised by:
  Dr. Mohammad Ali Khasawneh
Coordinator:
  Dr. Andi Asiz

## Slide 3: Outline
Introduction
Traffic Analysis
Soil Study
Geometric Design
Pavement Design
Intersection
Cost Estimation
Summary & Conclusion

## Slide 4: Introduction
Location
Objective
Methodology
Constraints

## Slide 5: Introduction
Project Area
Alhofuf western ring road is located between the start of 6614 route and ends 6446 route
Notes: As you can see in this figure, our project area is located in west of Alhofuf city.
It has boundary that closes from the pipeline and the railway
It starts from the north route 6614 and ends in the south route 6446

## Slide 6: Objectives
Finding the right path of the proposed road economically;
Analyzing and predicting traffic movements through the new highway;
Investigating the soil to neglect any land deformation after commencing the road construction;
Designing geometric alignments for the safety of the users;
Designing pavement layers that is suitable to the road; and
Designing a hydraulic system that facilitate the drainage of water on the road.

## Slide 7
Methodology
Geometric Design
Horizontal Alignment
Traffic Analysis
Vertical Alignment
Cost Estimation
Environmental
Pavement Structural Design
Soil Specification
Flexible Pavement
Drainage System
Environmental Assessment
Intersections

## Slide 8: Constraints
Establish road paths
Traffic Counting
Soil Testing
Geometric Design
Pavement Design
Environmental
Water Flow Management
Cost Estimation

## Slide 9: Alternatives
Alternatives # | Road length (km) | Elevation Gain/Loss | Max/Min Slope | Max. cut quantity (m3) | Max. fill quantity (m3)
Path A | 29.1 | +70 -67 | +10.4 -13.6% | 3,222,000 | 3,214,000
Path B | 24.3 | +64 -62 | +26.4 | 9,397,200 | 5,546,000
Path C | 26.8 | +88 -52 | +24.6 | 12,712,000 | 2,992,000
Alternatives # | Road length (km) | Elevation Gain/Loss | Max/Min Slope | Max. cut quantity (m3) | Max. fill quantity (m3)
Path A | 29.1 | +70 -67 |  | 3,222,000 | 3,214,000
Path B | 24.3 | +64 -62 |  | 9,397,200 | 5,546,000
Path C | 26.8 | +88 -52 |  | 12,712,000 | 2,992,000

## Slide 10: Traffic Analysis
Data Collection
Future Traffic Daily Volume
Design Speed
Road Capacity
# of Lanes

## Slide 11: Average Weekly Traffic Volume from Riyadh Rd to Airport
Chart: Riyadh Rd to Airport
| 18/10/2019. | 19/10/2019. | 20/10/2019. | 21/10/2019. | 22/10/2019. | 23/10/2019. | 24/10/2019.
PC | 529 | 665 | 618 | 677 | 722 | 499 | 724
Taxi | 166 | 98 | 67 | 97 | 189 | 170 | 250
PICK UP | 49 | 71 | 74 | 87 | 24 | 66 | 43
JEEP MODEL | 217 | 164 | 268 | 305 | 422 | 406 | 409
SMALL BUS | 12 | 7 | 14 | 13 | 31 | 27 | 36
BIG BUS | 6 | 14 | 12 | 19 | 18 | 22 | 15
TOTAL | 979 | 1019 | 1053 | 1198 | 1406 | 1190 | 1477
Traffic Analysis
[1]

## Slide 12: Average Weekly Traffic Volume from Airport to Riyadh Rd
Chart: Airport to Riyadh Rd
| 18/10/2019. | 19/10/2019. | 20/10/2019. | 21/10/2019. | 22/10/2019. | 23/10/2019. | 24/10/2019.
PC | 482 | 916 | 389 | 601 | 614 | 666 | 706
Taxi | 212 | 310 | 114 | 103 | 194 | 215 | 167
PICK UP | 66 | 88 | 38 | 48 | 95 | 36 | 58
JEEP MODEL | 201 | 170 | 187 | 346 | 329 | 499 | 439
SMALL BUS | 22 | 32 | 17 | 29 | 16 | 39 | 31
BIG BUS | 19 | 7 | 11 | 20 | 3 | 27 | 7
TOTAL | 1002 | 1523 | 756 | 1147 | 1251 | 1482 | 1408
Traffic Analysis
[1]

## Slide 13: Future traffic daily volume after 20yr (ADT)b.y
Type of Vehicle | (ADT)d.y | Gf | (ADT)b.y
PC | 1262 | 4% | 2765
TAXI | 337 | 4% | 738
PUCK UP | 122 | 4% | 267
JEEP MODEL | 624 | 4% | 1368
SMALL BUS | 47 | 4% | 85
BIG BUS | 30 | 3% | 55
TOTAL | 2422 |  | 5278
Traffic Analysis
[2]

## Slide 14: The equivalent future traffic daily volume
TYPE OF VEH. | FACTOR (K) | (ADT)d.y | (ADT)b.y (20y) | (AADT)b.y
PC | 1 | 1262 | 2765 | 2765
TAXI | 1 | 337 | 738 | 738
PUCK UP | 1.25 | 122 | 267 | 334
JEEP MODEL | 1.3 | 624 | 1368 | 1779
SMALL BUS | 1.3 | 47 | 85 | 111
BIG BUS | 2.25 | 30 | 55 | 124
TOTAL |  | 2422 | 5307 | 5885
Traffic Analysis
[2]

## Slide 15: Calculate the prevailing traffic volume in one direction
The design traffic volume in one direction as shown in the following equation:
Whereas:
Df = directional factor = (50%~70%)
The coefficient will be taken equal to (50%):
Traffic Analysis

## Slide 16: Design Speed
Road degree | Lower speed (Km/hr.) | Upper speed (Km/hr.)
Local | 30 | 50
Collector | 50 | 60
Arterial Highway | 80 | 100
Less disorder | 70 | 90
High disturbance | 50 | 60
Expressway | 90 | 120
Nature of the region | Speed (Km/hr.) |  | 
 | Urban Road | Secondary road | Rural Road
Plain area | 120 | 100 | 80
Rolling area | 100 | 80 | 60
According to that, the designed speed will be
100 km/h.
Traffic Analysis
[3]

## Slide 17: # of Lanes
For 1600 veh/h
The best road capacity regarding to guideline equal to 1600 veh/h.
Traffic Analysis
[12]

## Slide 18: Soil Profile

## Slide 19: Soil Classification Systems
AASHTO System
Unified Soil Classification System
Textural Classification
American Society of Testing Material
Soil Study

## Slide 20: Sieve Analysis Samples
Sample #1 |  | 
Liquid Limit L. L | Plastic Limit P. L | Plastic Index P. I
23% | 15% | 8%
Gravel % | Sand % | Silt & Clay %
20.7% | 16.7% | 62.6%
AASHTO Classification |  | 
A-4, silty soils |  | 
Unified Soil Classification System |  | 
CL, Gravely Lean Clay |  | 
Sample #2 |  | 
Liquid Limit L. L | Plastic Limit P. L | Plastic Index P. I
22% | 15% | 7%
Gravel % | Sand % | Silt & Clay %
21.3% | 10.2% | 68.5%
AASHTO Classification |  | 
A-4, silty soils |  | 
Unified Soil Classification System |  | 
CL-ML, Gravely Silty Clay |  | 
Sample #3 “Weakest” |  | 
Liquid Limit L. L | Plastic Limit P. L | Plastic Index P. I
20% | 12% | 8%
Gravel % | Sand % | Silt & Clay %
13.1% | 20.2% | 66.7%
AASHTO Classification |  | 
A-4, silty soils |  | 
Unified Soil Classification System |  | 
CL, Sandy lean clay |  | 
Sample #4 |  | 
Liquid Limit L. L | Plastic Limit P. L | Plastic Index P. I
30% | 25% | 5%
Gravel % | Sand % | Silt & Clay %
14.5% | 32.6% | 52.9%
AASHTO Classification |  | 
A-4, silty soils |  | 
Unified Soil Classification System |  | 
CL-ML, Sandy Silty clay |  | 
[5]

## Slide 21
Test | 1 |  | 2 |  | 3 | 
Blows | 10 |  | 30 |  | 65 | 
Volume of mould ( | 2133 |  | 2139 |  | 2136 | 
Mass of compacted specimen (g) | 4960 |  | 5099 |  | 5295 | 
Mass of soaked drained specimen (g) | 5067 |  | 5207 |  | 5355 | 
Water content (%) | 6.6 | 12 | 6.5 | 11.2 | 6.4 | 10.1
Density of compacted specimen | 2.325 |  | 2.384 |  | 2.479 | 
Density of soaked specimen | 2.376 |  | 2.434 |  | 2.507 | 
Dry density | 2.181 |  | 2.238 |  | 2.330 | 
Compaction % | 94.4 |  | 96.9 |  | 100.8 | 
Swell % | 0.48 | 0.48 | 0.38 |  | 0.25 | 
Test | 1 |  | 2 |  | 3 | 
Blows | 10 |  | 30 |  | 65 | 
 | 2133 |  | 2139 |  | 2136 | 
Mass of compacted specimen (g) | 4960 |  | 5099 |  | 5295 | 
Mass of soaked drained specimen (g) | 5067 |  | 5207 |  | 5355 | 
Water content (%) | 6.6 | 12 | 6.5 | 11.2 | 6.4 | 10.1
Density of compacted specimen | 2.325 |  | 2.384 |  | 2.479 | 
Density of soaked specimen | 2.376 |  | 2.434 |  | 2.507 | 
Dry density | 2.181 |  | 2.238 |  | 2.330 | 
Compaction % | 94.4 |  | 96.9 |  | 100.8 | 
Swell % | 0.48 | 0.48 | 0.38 |  | 0.25 | 
Proctor Test: MDD = 2.311 , OMC = 6.5%
Weight Calculation
Water Content Determination
Densities
Swelling Test
Soil Study
[5]

## Slide 22: Penetration Test
Chart: Penetration (mm)
| 0 | 0.64 | 1.27 | 1.91 | 2.54 | 3.18 | 3.81 | 4.45 | 5.08 | 7.62 | 10.16
10 Blows | 0 | 3.5 | 6.4 | 9 | 11.2 | 13.6 | 15 | 17 | 18.7 | 26.4 | 33
30 Blows | 0 | 7.5 | 13.6 | 18.5 | 23.2 | 27.1 | 30.8 | 35 | 37.9 | 49.5 | 59.4
65 Blows | 0 | 11 | 20.3 | 28.2 | 34.3 | 40.7 | 47.1 | 52.6 | 58.3 | 80.6 | 96.9
Soil Study
[5]

## Slide 23: CBR Calculation
Mould # | CBR @ 2.5 mm (%) | CBR @ 5 mm (%)
1 | 16 | 17.8
2 | 33.2 | 36.1
3 | 48.9 | 55.6
Chart: CBR @ 5 mm
| 2.181 | 2.238 | 2.33
CBR @ 5 mm (%) | 17.8 | 36.1 | 55.6
95% | 0 | 22.8
Cross 95% | 22.8 | 22.8
100% | 0 | 52.2
Cross 100% | 52.2 | 52.2
CBR value at 95% of MDD
= 22.8% @ 5 mm
Soil Study

## Slide 24: Horizontal Alignment
Horizontal Curve at Station 7+12
Horizontal Curve at Station 28+64
Horizontal Curve at Station 50+30
Horizontal Curve at Station 56+14

## Slide 25: Horizontal Alignment
25 horizontal curves
[1+00 = 500 m]
Using simple curve
SSD
PSD
Super Elevation

## Slide 26: Designed Horizontal Curve at Station 7+12

## Slide 27: Points On Horizontal at Station 7+12
Station (0+00) | Degree (Ɵ) | X (m) | Y (m) | L (m)
7+08 | 0 | 0 | 0 | 0
7+09 | 1.32 | 4.61 | 0.05 | 5
7+10 | 2.64 | 9.21 | 0.21 | 10
7+11 | 3.96 | 13.81 | 0.48 | 15
7+12 | 5.28 | 18.40 | 0.85 | 20
7+13 | 6.6 | 22.99 | 1.33 | 25
7+14 | 7.92 | 27.56 | 1.91 | 30
7+15 | 9.24 | 32.11 | 2.59 | 35
7+16 | 10.56 | 36.65 | 3.39 | 40
7+16.726 | 11.52 | 39.94 | 4.03 | 43.63
7+17.45 | 12.48 | 43.22 | 4.73 | 47.27

## Slide 28: Designed Horizontal Curve at Station 28+64
Horizontal Alignment
28

## Slide 29: Points On Horizontal at Station 28+64
Horizontal Alignment
Station (0+00) | Degree (Ɵ) | X (m) | Y (m) | L (m)
28+40 | 0 | 0 | 0 | 0
28+46 | 6.336 | 27.59 | 1.53 | 30
28+52 | 12.672 | 54.84 | 6.09 | 60
28+58 | 19.008 | 81.43 | 13.63 | 90
28+64 | 25.344 | 107.01 | 24.06 | 120
28+70 | 31.68 | 131.3 | 37.25 | 150
28+76 | 38.016 | 153.97 | 53.04 | 180
28+82 | 44.352 | 174.77 | 71.24 | 210
28+87.23 | 49.875 | 191.16 | 88.88 | 236.15
28+91.23 | 54.1 | 202.51 | 103.41 | 256.16

## Slide 30: Designed Horizontal Curve at Station 50+30
Horizontal Alignment
30

## Slide 31: Points On Horizontal at Station 50+30
Horizontal Alignment
Station (0+00) | Degree (Ɵ) | Y (m) | X (m) | L (m)
50+00 | 0 | 0 | 0 | 0
50+06 | 3.96 | 0.95 | 27.62 | 30
50+12 | 7.92 | 3.82 | 55.12 | 60
50+18 | 11.88 | 8.57 | 82.35 | 90
50+24 | 15.84 | 15.19 | 109.18 | 120
50+30 | 19.8 | 23.65 | 135.50 | 150
50+36 | 23.76 | 33.90 | 161.16 | 180
50+42 | 27.72 | 45.91 | 186.06 | 210
50+48 | 31.68 | 59.60 | 210.07 | 240
50+54 | 35.64 | 64.53 | 217.86 | 270
50+60 | 39.6 | 80.38 | 240.50 | 300
50+66 | 43.56 | 97.75 | 262.00 | 330
50+66.616 | 43.97 | 112.10 | 277.70 | 333.08
50+72.288 | 47.71 | 130.85 | 295.9 | 361.44

## Slide 32: Designed Horizontal Curve at Station 56+14

## Slide 33: Points On Horizontal at Station 56+14
Station (0+00) | Degree (Ɵ) | X (m) | Y (m) | L (m)
56+06 | 0 | 0 | 0 | 0
56+08 | 4.4997 | 9.414465106 | 0.369870656 | 10
56+10 | 8.9994 | 18.77089464 | 1.477202554 | 20
56+12 | 13.4991 | 28.01161079 | 3.315169533 | 30
56+14 | 17.9988 | 37.07964905 | 5.872441425 | 40
56+16 | 22.4985 | 45.91910941 | 9.133253901 | 50
56+18 | 26.9982 | 54.47550093 | 13.07750565 | 60
56+19.988 | 31.4979 | 62.69607762 | 17.68088228 | 69.94
56+21.18 | 33.395 | 66.04894605 | 19.81249217 | 75.9

## Slide 34: Vertical Alignment
Fundamentals
Types of Vertical Curves
Considerations
Vertical Curve Designs

## Slide 35: Vertical Alignment
12 vertical curves design
Using 4 types of curves
SSD
PSD
K-value
HSD
CSD
ASD

## Slide 36: Types of Vertical Curves
Vertical Alignment
[3]

## Slide 37: Point On Curve for Crest at Station [2+12]
Vertical Alignment
Point | X | Y(m) | Tangent E | E (m)
VPC | 0 | 0 | 130 | 130
1 | 40 | 0.217636 | 132.756 | 132.5384
2 | 80 | 0.870545 | 135.512 | 134.6415
3 | 120 | 1.958727 | 138.268 | 136.3093
4 | 160 | 3.482182 | 141.024 | 137.5418
5 | 200 | 5.440909 | 143.78 | 138.3391
6 | 240 | 7.834909 | 146.536 | 138.7011
7 | 280 | 10.66418 | 149.292 | 138.6278
8 | 320 | 13.92873 | 152.048 | 138.1193
9 | 360 | 17.62855 | 154.804 | 137.1755
10 | 400 | 21.76364 | 157.56 | 135.7964
VPT | 440 | 26.334 | 160.316 | 133.982
37

## Slide 38: Crest Vertical Curve Profile
Vertical Alignment

## Slide 39: Point On Curve for Crest at Station [32+12]
Point | X | Y | Tangent E | E
VPC | 0 | 0 | 190 | 190
1 | 15 | 0.021375 | 188.6425 | 188.6211
2 | 30 | 0.0855 | 187.285 | 187.1995
3 | 45 | 0.192375 | 185.9275 | 185.7351
4 | 60 | 0.342 | 184.57 | 184.228
VPI | 75 | 0.534375 | 183.2125 | 182.6781
6 | 90 | 0.7695 | 181.855 | 181.0855
7 | 105 | 1.047375 | 180.4975 | 179.4501
8 | 120 | 1.368 | 179.14 | 177.772
9 | 135 | 1.731375 | 177.7825 | 176.0511
VPT | 150 | 2.1375 | 176.425 | 174.2875
Vertical Alignment
Point On Curve for Crest at Station [32+12]

## Slide 40
Vertical Alignment

## Slide 41: Point On Curve for Sag At Station [36+06]
Vertical Alignment
41
Point | X (m) | Y(m) | Tangent E | E (m)
VPC | 0 | 0 | 121 | 121
1 | 50 | 0.2155 | 117.555 | 117.7705
2 | 100 | 0.862 | 114.11 | 114.972
3 | 150 | 1.9395 | 110.665 | 112.6045
4 | 200 | 3.448 | 107.22 | 110.668
5 | 250 | 5.3875 | 103.775 | 109.1625
6 | 300 | 7.758 | 100.33 | 108.088
7 | 350 | 10.5595 | 96.885 | 107.4445
8 | 400 | 13.792 | 93.44 | 107.232
9 | 450 | 17.4555 | 89.995 | 107.4505
VPT | 500 | 21.55 | 86.55 | 108.1

## Slide 42: Sag Vertical Curve Profile
Vertical Alignment

## Slide 43: Point On Curve for Sag At Station [26+10]
Point | X | Y | Tangent E | E
VPC | 0 | 0 | 188 | 188
1 | 15 | 0.01815 | 186.2795 | 186.2977
2 | 30 | 0.0726 | 184.559 | 184.6316
3 | 45 | 0.16335 | 182.8385 | 183.0019
4 | 60 | 0.2904 | 181.118 | 181.4084
VPI | 75 | 0.45375 | 179.3975 | 179.8513
6 | 90 | 0.6534 | 177.677 | 178.3304
7 | 105 | 0.88935 | 175.9565 | 176.8459
8 | 120 | 1.1616 | 174.236 | 175.3976
9 | 135 | 1.47015 | 172.5155 | 173.9857
VPT | 150 | 1.815 | 170.795 | 172.61
Vertical Alignment
Point On Curve for Crest at Station [26+10]

## Slide 44
Vertical Alignment

## Slide 45: Pavement Design

## Slide 46: Pavement Design Type
Pavement Design

## Slide 47: Design Method “AASHTO”
Pavement Design

## Slide 48: Sections of The Highway Station (42+00 to 44+00)
Station (42+00 to 44+00)
Pavement Design

## Slide 49: “AASHTO” Design Method
Steps | Design Parameter | Equation | Result
1 | Reliability / Std. Dev. | - | 85% ¦ 0.45
2 | ESAL |  | 
3 | Roadbed Soil | - | Mr = 7,000 psi
4 | PSI | Pi – Pt = PSI | 2
Steps | Design Parameter | Equation | Result
1 | Reliability / Std. Dev. | - | 85% ¦ 0.45
2 | ESAL |  | 
3 | Roadbed Soil | - | Mr = 7,000 psi
4 | PSI | Pi – Pt = PSI | 2
Pavement Design

## Slide 50: Pavement coefficients ()
Layer | (AC) | B.C | Sub.B
CBR% | Marshall (Stability) (1900 lbs.) | 85% | 40%
(psi) | Modulus (40,000 psi) | 29,500 psi | 17,000 psi
 | 0.42 | 0.135 | 0.12
Layer | (AC) | B.C | Sub.B
CBR% | Marshall (Stability) (1900 lbs.) | 85% | 40%
 | Modulus (40,000 psi) | 29,500 psi | 17,000 psi
 | 0.42 | 0.135 | 0.12
Pavement Design
Notes: a_1 = It is the coefficient of the surface layer (asphalt layer) so it will depend on the properties of the asphalt mixture and from the table we find that:
a_1=0.42
M_r = 42,000 psi
As for the base layer and the auxiliary foundation, finding the coefficients of the layer and the regression coefficient will depend on the value of the CBR, and here it is imposed by the engineer designed to suit the specifications of each layer, and the following table shows the imposed CBR values, the class coefficient values,

## Slide 51: Drainage Coefficient (), ():
Layer | Base Course | Sub base
Water removed from 100%-50% saturation | 1 day | 1 day
Quality of Drainage | Good | Good
 | 1.15 | 1.15
Layer | Base Course | Sub base
Water removed from 100%-50% saturation | 1 day | 1 day
Quality of Drainage | Good | Good
 | 1.15 | 1.15
Pavement Design

## Slide 52: Structural Number
SN |  |  | 
Value | 3.0 | 3.8 | 4.9
SN |  |  | 
Value | 3.0 | 3.8 | 4.9
Using the monograph in the following figure we get the following values:
Pavement Design
Monograph [12]

## Slide 53: Layers Thickness Calculation
Asphalt Course
And since the asphalt layer is considered expensive, this thickness will be compensated for in the lower foundation layers.
Use D1= 5.9 in =15cm.
Base Course
According to road engineer advise, the minimum thickness should be 9.84 in for the base
Use D2 = 9.84 in or 25 cm, because sub-base will compensate
Sub – Base
Use D3= 9.84 in or 25 cm
Pavement Design

## Slide 54
Horizontal Curve Pavement Cross-section
Pavement Cross-section Design
12%
Pavement Design

## Slide 55: Drainage System
Notes: design

## Slide 56: Drainage System
Drainage System
Insignificant elevation differences
The road will be cut to sections which include 1Km linear distance and width with 40m (A = 40,000 )
Design Period is 50 years
Mean Intensity; for 2H duration and 10 year return period
Topography Map[4]

## Slide 57: Drainage System
Then the design intensity for 50 years period and 1Hr duration is 145.3mm/hr.
Chart: Duration (Mean)
| 1H | 2H | 6H | 12H | 24H
2year | 45.17 | 30.55 | 12.89 | 7.14 | 3.91
5year | 64.19 | 44.6 | 21.36 | 12.02 | 0.44
10year | 76.79 | 53.9 | 26.97 | 15.25 | 0.11
50year | 104.51 | 74.36 | 39.31 | 22.36 | 11.79
100year | 116.23 | 83.02 | 44.53 | 25.37 | 13.35
Drainage System

## Slide 58: Drainage System
Hydraulic Design:
/sec) Eq(8.3)
Maximum Flow
→
Drainage Gutter[15]
Drainage System

## Slide 59: Road Intersection

## Slide 60: Road Intersection
The intersection is considered to be the area of changing direction of movement for vehicles and the area of collection and dispersion for these vehicles.
The intersection is a meeting point or crossing two or more roads at a certain level.
The intersection is a difficult area for drivers.
The main task of the intersection is to change direction or crossing.
Road Intersection

## Slide 61: Intersections on the Road
Intersection | Name of road | Station
1 | Dammam-Alhofuf Rd. | [0+00]
2 | Mekkah Almukaramah Interchange | [20+60]
3 | Industrial City of Alahsa- Riyadh Rd. | [51+60]
4 | Livestock Market-Almubaraz Rd. | [58+00]
Road Intersection

## Slide 62: Road Intersections
Diamond Interchange
(Google Earth, 2020)
Road Intersection
(RFFLO5, 2020)

## Slide 63: Intersection Path Suggestion Station [20+60]
After analyzing the movement of the two roads, we suggested the following intersection path the figure below:
Station [20+60]
Suggested Intersection

## Slide 64: Traffic Analysis
Then determine factor Fhv, according to HCM (High-Capacity Manual):
Fhv of PC = 1.00
Fhv of Bus = 1.5
Fhv of Trailer = 2.00
Path | PC | Bus | Trailer | Total
1 | 712 | 12 | 14 | 738
2 | 608 | 18 | 32 | 658
3 | 754 | 29 | 28 | 811
4 | 722 | 38 | 23 | 783
Road Intersection

## Slide 65: Determine the number of lanes
Based on the PCE values, the maximum value was = 844, and regarding to HCM, the capacity equal to 608 pc/lane, in urban compact, so:
Path | PCE | No. | Uses No.
1 | 753 | 1.23 | 2
2 | 698 | 1.14 | 2
3 | 844 | 1.39 | 2
4 | 822 | 1.35 | 2
Road Intersection

## Slide 66: Cost Estimation

## Slide 67: Cost Estimation
# | Item | Total [SR]
1 | Cutting and back filling the natural land. | 13,920,000
2 | Supply and install sub-base layer | 6,525,000
3 | Supply and install Base-course layer, | 5,220,000
4 | Supply and install MC1 layer | 1,160,000
5 | Supply and install asphalt layer | 27,840,000

## Slide 68: Cost Estimation
# | Item | Total [SR]
6 | Supply and install RC2 layer | 1,160,000
7 | Supply and install asphalt layer | 24,360,000
8 | Installing white solid lane lines | 2,088,000
9 | Supply and install new jersey barriers | 3,222,222
10 | Supply and install road fences | 6,000,000

## Slide 69
Quotation | 
Total cost of the material | 91,495,222
Terms of management cost | (1.5%)
Balance value | (10%)
Market taxes | (15%)
Total cost of the project | 117,477,577.7 SR
Cost Estimation

## Slide 70: Summary
Consider the economically influencing fields.
The study was determining the, geographical location, studying the topography, and appropriate path.
The containing statistics of number of vehicles were taken from Ministry of Transport .
The road body was studied geometrically
The results of the soil were determined.
The paving layers were determining the structural section.
The 29 Km road was determining the construction of road market in Saudi Arabia.

## Slide 71: Conclusion
Determining the road path.
Determine the number of lanes.
Investigating the soil.
Designing the geometric alignments.
Determining the thicknesses of the road pavement.
Designing the drainage of the road.
Introduce and designing an intersection.
Estimated the cost.

## Slide 72
Month | 9 | 9 | 9 | 9 | 10 | 10 | 10 | 10 | 11 | 11 | 11 | 11 | 12 | 12 | 12 | 12 | 1
Week | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17
Data Collection |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Proposal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Layout |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Preliminary Design |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Hand calculations |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Structural Design and Analysis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Cost Estimation |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Final Report |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Final Report Correction |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Final Presentation |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 73: References
Ministry of Transportation (2019), Traffic Data, Ministry of Transportation Official.
(1995). AASHTO provisional standards. Washington, D.C: American Association of State Highway and Transportation Officials
Khasawneh, M.(2020). Transportation Engineering. Course materials, Prince Mohammed bin Fahad University.
Contour Map Creator (2020), Topography Area of The Proposed Road, URL: https://contour mapcreator.urgr8.ch/
Testing House (2020), Soil Data, Acquired on 30 September 2020 [Location: Saudi Arabia, Alhofuf, Salad Al-Din Ayyubi Street]
Ayadat, T.(2019). Introduction to Geotechnical Engineering. Course materials, Prince Mohammed bin Fahad University
Hogentogler, C.A.; Terzaghi, K. (May 1929). "Interrelationship of load, road and subgrade". Public Roads: 37–64.
Lowell, U. (2015, January). 14.330 Soil Mechanics Soil Classification. Lecture presented at Slide 25.
Almasre, H., Civil Engineer, Dammam, Kingdom of Saudi Arabia.
Traffic and Highway Engineering, Nicholas J. Garber, Lester A. Hoel, 2011 Edition
Institute, N. (2006). Geotechnical Aspects of Pavements. In U.S. Department of Transportation: Federal Highway Administration (pp. 1-11). New Jersey, WA: FHWA NHI-05-037.
Garber, N. J., &amp; Hoel, L. A. (2020). Traffic and highway engineering. Australia, .: Cengage.
Municipality of Alahsa (2013), Rainfall Data, [Location: Saudi Arabia, Al Mubaraz, 364421]
Roy, S. (2018, October 10). CALIFORNIA BEARING RATIO TEST [Photograph].
Consultant, R. (2020, November). Fundamental of Road Construction Maintanace Program [Photograph].
Mahajan, M. (2020, February 26). Https://civiconcepts.com/2020/02/what-is-pavement-types-of-pavement-road-construction-layers/ [Photograph].
73

## Slide 74
74

## Slide 75
75